- Classic Article

The effect of ceramic surface treatment on bonding to densely sintered alumina ceramic

Luiz Felipe Valandro DDS, MSca, Alvaro Della Bona DDS, MMedSci, PhDb, , , Marco Antonio Bottino DDS, PhDc and Maximiliano Piero Neisser DDS, MSc, PhDd 
aProfessor, Department of Restorative Dentistry, School of Dentistry, Federal University of Santa Maria
bProfessor and Research Coordinator, School of Dentistry, University of Passo Fundo
cProfessor, Department of Dental Materials and Prosthodontics, Sao Paulo State University at Sao Jose dos Campos
dProfessor, Department of Dental Materials and Prosthodontics, Sao Paulo State University at Sao José dos Campos 
Federal University of Santa Maria, Rio Grande do Sul, Brazil; University of Passo Fundo, Rio Grande do Sul, Brazil; Sao Paulo State University at Sao Jose dos Campos, Brazil.  Available online 9 March 2005.

- Statement of problem

Ceramic surface treatment is crucial for bonding to resin. High crystalline ceramics are poorly conditioned using traditional procedures.

- Purpose

The purpose of this study was to evaluate the effect of silica coating on a densely sintered alumina ceramic relative to its bond strength to composite, using a resin luting agent.

- Material and methods

Blocks (6 × 6 × 5 mm) of ceramic and composite were made. The ceramic (Procera AllCeram) surfaces were polished, and the blocks were divided into 3 groups (n = 5): SB, airborne-particle abrasion with 110-μm Al2O3; RS, silica coating using Rocatec System; and CS, silica coating using CoJet System. The treated ceramic blocks were luted to the composite (W3D Master) blocks using a resin luting agent (Panavia F). Specimens were stored in distilled water at 37°C for 7 days and then cut in 2 axes, x and y, to obtain specimens with a bonding area of approximately 0.6 mm2 (n = 30). The specimens were loaded to failure in tension in a universal testing machine, and data were statistically analyzed using a randomized complete block design analysis of variance and Tukey's test (α=.05). Fractured surfaces were examined using light microscopy and scanning electron microscopy to determine the type of failure. Energy-dispersive spectroscopy was used for surface compositional analysis.

- Results

Mean bond strength values (MPa) of Groups RS (17.1 ± 3.9) (P=.00015) and CS (18.5 ± 4.7) (P=.00012) were significantly higher than the values of Group SB (12.7 ± 2.6). There was no statistical difference between Groups RS and CS. All failures occurred at the adhesive zone.

- Conclusion

Tribochemical silica coating systems increased the tensile bond strength values between Panavia F and Procera AllCeram ceramic.

- Article Outline

Material and methods

Results

Discussion

Conclusions

References

Clinical implications

Silica coating of densely sintered alumina ceramic restorations increased the bond strength to the resin luting agent tested.

With the increase of aluminum oxide content (Al2O3) in feldspathic ceramics, there has been a significant improvement in the mechanical properties of these materials, allowing metal-free restorations to be used more predictably.1 Procera AllCeram (Nobel Biocare, Stockholm, Sweden) is a high-strength ceramic material with a highly dense, sintered Al2O3 content (99.9% of Al2O3) with a negligible glassy phase.2

The ceramics with high crystalline content (aluminum and/or zirconium oxides) have demonstrated better clinical results than feldspar-, leucite-, and lithium disilicate–based ceramics.3, 4, 5, 6 and 7 In fact, increasing the mechanical strength, by increasing the crystalline content and decreasing the glass content, results in an acid-resistant ceramic whereby any type of acid treatment produces insufficient surface changes for adequate bonding to resin.2, 8, 9, 10, 11 and 12

However, the bonding of resin composites to feldspar-, leucite-, and lithium disilicate–based ceramics is well established. Hydrofluoric acid attacks the glass phase producing a retentive surface for micromechanical bonding, and the silane coupling agent promotes a chemical bond between the silica of these ceramics and the methacrylate groups of the resin.11, 12, 13, 14, 15, 16, 17 and 18 The silica coating process9, 10, 14 and 16 is based on similar adhesive principles and appears to be a promising method for treating high crystalline ceramics.

Some studies have evaluated the effect of silica coating on the bond strength of acid-resistant ceramics bonded to resin luting agents.2, 19, 20, 21 and 22 In addition, several authors have criticized some bond strength testing methods and suggested the use of a tensile test methodology to evaluate the bond strength of resin to ceramic.23, 24, 25, 26, 27, 28 and 29

Nevertheless, little information is available on the effect of bonding silica-coated high-crystalline ceramics to resin luting agents containing phosphate monomers. Therefore, the purpose of this study was to test the hypothesis that silica-coating a densely sintered alumina ceramic increases the bond strength to a resin luting agent containing phosphate monomers.

- Material and methods

Fifteen blocks (6 mm × 6 mm × 5 mm) of densely sintered alumina ceramic (Procera AllCeram (PR); Nobel Biocare, Göteborg, Sweden) were obtained from the manufacturer. The ceramic surface was polished with 1200-grit metallographic paper (3M ESPE, St. Paul, Minn) using a polishing machine (Labpol 8-12; Extec, Enfield, Conn). Each ceramic block was duplicated in resin composite (batch no. 010/03; W3D Master; Wilcos, Petrópolis, Brazil) using a mold made of an addition silicone impression material (Elite HD, batch no. Bo1.01.B; Zhermack, Badia Polesine, Rovigo, Italy). Incremental layers of resin composite (2 mm) were condensed into the mold and polymerized for 40 seconds (XL 3000; 3M ESPE; light output = 500 mW/cm2) to fill the mold. One resin composite (RC) block was fabricated for each ceramic block.

The ceramic blocks were randomly divided into 3 groups and treated as follows. For Group SB specimens, the ceramic surface was treated using an airborne-particle abrasion system with 110-μm aluminum oxide particles (MicroEtcher; Danville Engineering, San Ramon, Calif). The abrasion was applied perpendicular to the surface at a distance of 10 mm for 15 seconds and at a pressure of 2.8 bars.

For Group RS specimens the Rocatec System (batch no. 363; 3M ESPE) was used to treat the ceramic surface. The manufacturer's recommendations were followed for the use of the Rocatec-Pre, Rocatec-Plus, and Rocatec-Sil. The Rocatec-Pre uses airborne-particle abrasion with 110-μm Al2O3 particles employing the same abrasion parameters used with the group SB. The Rocatec-Plus consists of airborne-particle abrasion using 110-μm Al2O3 particles modified by silica with abrasion parameters equal to the Rocatec-Pre. The Rocatec-Sil was applied onto the silica-coated surface.20, 30, 31, 32 and 33

For Group CS the ceramic surface was treated with airborne-particle abrasion with 30-μm Al2O3 particles modified by silica (CoJet System, batch no. 118484; 3M ESPE), using the same abrasion parameters used with the SB and RS Groups. The surfaces were coated with a silane coupling agent (ESPE-Sil; 3M ESPE), which was allowed to air dry for 5 minutes.34 and 35

One additional specimen from each Group was sputter-coated with gold-palladium (Hummer II Sputter Coater; Technics Inc, Alexandria, Va) for 3 minutes, at a current of 10 mA, and vacuum of 130 mTorr. The surface topography of the specimens was examined using a scanning electron microscope (JSM 6400; Jeol Ltd, Tokyo, Japan).12 Some CoJet-treated ceramic specimens were analyzed for the silica content. Silica mappings were generated using energy-dispersive spectroscopy (EDS) at 20 Kv. Representative images and spectra were recorded.

Each treated ceramic block was bonded to a composite block using a resin luting system (batch no. 107AF, Dual-Cure Dental Adhesive System Panavia F; Kuraray Co, Okayama, Japan) according to the manufacturer's instructions. The ceramic-resin luting agent-composite set was placed under a load of 750 g in a press (EMIC PCE 10D; EMIC, São José dos Pinhais, Brazil).30, 31, 32 and 33 The excess resin luting agent was removed with a brush. The resin luting agent was polymerized (XL 3000) for 40 seconds on each side of the block.36 An oxygen inhibitor (Oxyguard; Kuraray Co) was applied on the resin luting agent layer for 10 minutes before removing the blocks from the press. The blocks were washed with air-water spray and stored in distilled water at 37°C for 7 days.

The blocks were bonded with cyanoacrylate (Super Bonder gel; Loctite Ltda, São Paulo, Brazil) to a metal base, which was attached to a low-speed, automatic precision cutting machine (Minitom; Struers, Copenhagen, Denmark) (Fig. 1, A). Slices approximately 0.8 mm thick were obtained using a slow-speed diamond wheel saw (batch no. 7016; KG Sorensen, Barueri, Brazil) under water cooling (Fig. 1, B). The peripheral slices were discarded because the results could be influenced by either an excess or an insufficient amount of resin luting agent at the interface.11, 37 and 38 Nontrimmed specimens were obtained directly from the cutting machine, meaning neither polishing nor finishing was performed. This procedure was used to avoid stress concentration at the adhesive interface by polishing materials with different elastic moduli.11 Six nontrimmed bar-shaped specimens with a bonding area of approximately 0.6 mm2 were obtained per block (n = 30) (Fig. 2, B).11, 39, 40 and 41

|  | Display Full Size version of this image (15K) |  | Fig. 1. A, The block was glued to metal base attached to cutting machine. B, Three slices (±0.8 mm thick) were obtained per block. | Display Full Size version of this image (16K) |  |
| --- | --- | --- | --- | --- | --- |

Fig. 2. (A) The slices were cut; (B) 6 inner specimens were used for tensile bond strength testing. Asterisk indicates adhesive zone as described by Della Bona et al.11

The specimens were glued with cyanoacrylate to an adapted caliper, parallel to its long axis, thus minimizing the bending forces in the adhesive zone during microtensile testing. This apparatus was attached to a universal testing machine (EMIC DL-1000; EMIC), and the specimens were loaded in tension to failure at a crosshead screw speed of 1 mm/min.11 and 40

Bond strength (σ) values were calculated using σ = L/A, where L is the load at failure and A is the adhesive area measured using a digital caliper (Mitutoyo, Tokyo, Japan) prior to testing.11 The results were analyzed using a randomized complete block design analysis of variance (ANOVA) and Tukey's test (α=.05) and statistical software (Statistix 8.0 for Windows; Analytical Software Inc, Tallahassee, Fla). Fractured surfaces were observed using light microscopy (Zeiss MC 80 DX; Carl Zeiss, Jena, Germany) and scanning electron microscopy (SEM) (JEOL-JSM-T330A; Jeol Ltd) to determine the type of failure, which was classified as cohesive or adhesive within any of the substrates or interfaces.

- Results

The randomized complete block design ANOVA is described in Table I, showing that there were significant differences among groups. The mean bond strength values and standard deviations are presented in Table II. The mean bond strength values of Groups RS and CS were not significantly different (P=.25), but the mean values of these groups were significantly higher than the mean value of Group SB (P=.0001). Representative SEM images of treated Procera AllCeram ceramic specimens are shown in Figure 3. Examination of the ceramic surfaces treated with both Rocatec-Plus and CoJet-Sand (Fig. 3) showed a deposition of particles onto the surface, which was different from the rough surface observed in the specimens from Group SB (Fig. 3, A). Figure 3, D, shows a silica mapping image based on EDS analysis of the silica-coated surface of Procera AllCeram. The examination of the fractured surfaces revealed that all failures occurred at the adhesive zone. All failures were cohesive fractures at the resin luting agent-ceramic interface (Fig. 4, Fig. 5 and Fig. 6).

Table I.

Randomized complete block design ANOVA

| SBRSCSTukeyMean values*12.7a17.1b18.5b3.402Standard deviation2.63.94.7FPR577.7315.547B484.321.074r×B20418.8920.944Surface treatment2550.76275.37822.36.0001Error58714.3012.315Total891845.98df, Degrees of freedom; SS, sum square; MS, mean square; B, block; r- repetitions.Source Table II. Mean bond strength values and standard deviation (MPa) of experimental groups and critical value for comparison | df |
| --- | --- |

SSMSSB, Airborne-particle abrasion with 110-μm Al2O3; RS, silica coating using Rocatec System; CS, silica coating using CoJet System.
* Different superscript letters indicate statistical difference, P<.05. Display Full Size version of this image (201K)Fig. 3. Representative SEM images of treated ceramic surfaces: A, airborne-particle abrasion with 110-μm Al2O3, ceramic surface treatment used for specimens in Group SB (original magnification ×2000); B, silica coating using Rocatec System, ceramic surface treatment used for specimens in Group RS (original magnification ×2000); C, silica coating using CoJet System, ceramic surface treatment used for specimens in Group CS (original magnification ×2000); D, EDS silica mapping for the silica-coated ceramic surface from Group CS; white spots are silica (original magnification ×100).

|  | Display Full Size version of this image (95K) |
| --- | --- |

Fig. 4. Representative SEM images of the fractured surface from specimens of Group SB. Area within the white square (A) is magnified in B (asterisk represents resin cement; spade symbol represents ceramic) (original magnifications: A, ×100; B, ×5000).

|  | Display Full Size version of this image (90K) |
| --- | --- |

Fig. 5. Representative SEM images of the fractured surface from specimens of Group RS. Area within the white square (A) is magnified in B (asterisk represents resin cement; spade symbol represents ceramic) (original magnifications: A, ×100; B, ×5000).

|  | Display Full Size version of this image (86K) |
| --- | --- |

Fig. 6. Representative SEM images of the fractured surface from specimens of Group CS. Area within the white square (A) is magnified in B (asterisk represents resin cement; spade symbol represents ceramic) (original magnifications: A, ×100; B, ×5000).

- Discussion

The results of this study confirmed the hypothesis that silica coating a densely sintered alumina ceramic increases the bond strength to a resin luting agent containing phosphate monomers. When a scientific investigation proposes to test the bond between an adhesive and an adherent, one of the essential aspects is the test method employed to measure the bond strength at the interface. In vitro bond strength tests, such as tensile or shear testing, are based on the application of a load to generate stress in the specimens until fracture occurs. Hence, for the test to produce adequate bond strength values between an adhesive system and a substrate, it is crucial that the bonding interface be the most stressed region, regardless of the test being employed.23, 24, 25 and 27

Many investigators, using stress distribution analyses, have reported that some bond strength tests do not appropriately stress the interfacial zone.23, 24, 25, 27, 28 and 38 In fact, shear tests have been criticized for the development of nonhomogeneous stress distributions in the bonding interface, inducing either an underestimation or a misinterpretation of the results, since the failure often starts in one of the substrates and not at the adhesive zone.23, 24, 25, 27, 28 and 38

Although conventional tensile tests also present some limitations, such as the difficulty of specimen alignment and the tendency of a heterogeneous stress distribution at the adhesive interface,23 and 38 this type of test may be used because it provides information about the overall bond strength.15, 16 and 41 The microtensile test, on the other hand, allows for an appropriate alignment of the specimens, and a more homogeneous distribution of stress, in addition to a more sensitive comparison or evaluation of bond strengths that are similar.11 As all of the specimens failed within the adhesive zone, the mean values reported are representative measurements of the tensile bond strength for the materials studied.11 and 29

Based on Della Bona et al,11 the adhesion zone in this study consists of the following: the interfacial region between the resin luting agent and the resin composite within which molecular interaction and chemical bonding occur, the resin luting agent, and the interfacial region between the resin luting agent and the dental ceramic. The latter includes the surface region treated with airborne-particle abrasion and/or coated with silica particles and silane such that micromechanical and/or chemical bonding occurs (Fig. 2, B).

Fracture surfaces were examined using light and scanning electron microscopy. SEM analysis provided more detailed information on the fracture events than the optical microscopy. Representative fracture surfaces are shown in Fig. 4, Fig. 5 and Fig. 6. It can be observed that the failure type for all groups was similar. Cohesive fracture always occurred within the adhesive zone at the resin luting agent-ceramic interface. Yet some authors suggested that fractographic analysis of the fracture surfaces provides qualitative information on the fracture process and should accompany the bond strength studies.11, 15, 26 and 29

The tribochemical silica coating systems increased the bond strength between the ceramic material and the resin luting agent studied. This result may be explained by 3 mechanisms: the creation of a topographic pattern allowing for micromechanical bonding to resin; the chemical bond between the silica-coated ceramic surface and the silane agent (y-methacryloxypropyltrimethoxysilane), and the latter to the resin material; and the chemical bond between the MDP phosphate monomers (10-methacryloxydecyl-dihydrogen-phosphate) and the aluminum oxides.32 Both the Rocatec (Fig. 3, B) and the CoJet (Fig. 3, C) systems produced a silica-coated ceramic surface, which was confirmed using silica mapping (Fig. 3, D). The silica coating systems created a silica layer on the ceramic surface because of the high-speed surface impact of the alumina particles modified by silica. It has been reported that the airborne particles can penetrate up to 15 μm into the ceramic and metal substrates.21

Kern and Thompson19 observed an increase in the silica content on the surface of In-Ceram ceramic, from 15.8% to 19.7%, after treatment with the Rocatec-Plus system, suggesting that this surface treatment could improve the bond strength to resin, which was later reported by other studies.8, 10 and 30 The CoJet and the Rocatec systems use similar methods for silica coating. The CoJet is a more versatile method for clinical procedures, such as the direct repair of fractured metal-ceramic and metal-free ceramic restorations using resin composite, and adhesive cementation. The Rocatec system is better suited for laboratory use. Yet, both systems employ silicatization and silanization of the substrate.34 and 35 Some studies reported that the mean bond strength values of glass-infiltrated aluminous ceramics bonded to resin increased after silica-coating, compared to airborne-particle abrasion with Al2O3 particles or hydrofluoric acid treatments.2, 8, 9 and 10

The ceramics can be classified as either acid-sensitive or acid-resistant, according to the degree of surface degradation with hydrofluoric acid (HF). Acid-sensitive ceramics, feldspar-, leucite- and lithium disilicate-based ceramics, are quickly etched by HF, resulting in micromechanical retentive ceramic surfaces. Acid-resistant ceramics, glass-infiltrated alumina and zirconia ceramic systems, densely sintered alumina ceramics, and yttrium-oxide-partially-stabilized zirconia ceramics do not demonstrate much surface degradation by HF etching, preventing a reliable micromechanical bond to resin.

The chemical bond to ceramic substrates can, therefore, be determined by the presence of silica in the ceramic composition.14 Although acids etch mainly the glassy phase, removing some silica from the surface to create a retentive topography for micromechanical bonding does not interfere with silanes producing a chemical bond with the remaining silica.14 Furthermore, the silane is bifunctional, also promoting a chemical bond to resinous materials via a cross-linkage with methacrylate groups. Most silane coupling agents also increase the substrate surface energy and improve the surface wettability to resins.11, 12, 13, 14, 15, 16, 17 and 18 The silica-silane chemical bond can occur with acid-resistant ceramics, provided that the silica coating of the ceramic surface is used. Kern and Thompson16 observed that the silane from Rocatec-Sil produced a chemical bond to a silica-coated glass-infiltrated alumina ceramic material (In-Ceram). Such a bond was negligible without silica coating, suggesting that silicatization and silanization procedures are essential to promote bonding between resin and the In-Ceram ceramic.

The Procera AllCeram ceramic material contains 99% aluminum oxide, characterizing an acid-resistant ceramic.2, 20 and 33 Yet, other studies of acid-resistant ceramics bonded to resins reported higher bond strength values when a resin luting agent containing phosphate monomers was used, which corroborates the results of the present study, suggesting that the association of silica coating, silanization, and resins containing phosphate monomers produced the highest bond strength values for acid-resistant ceramic materials bonded to resin.10, 22, 30, 31, 32 and 33 The results are relevant to the materials and procedures used in the present study. Future studies should examine the effect of silica coating on the bond strength to other high-crystalline content ceramics.

- Conclusions

Tribochemical silica coating systems (Rocatec and CoJet) significantly increased the mean bond strength values between a densely sintered alumina ceramic material (Procera AllCeram) and a resin luting agent containing phosphate monomers, confirming the study hypothesis.

- References

1 J. Tinschert, D. Zwez, R. Marx and K.J. Anusavice, Structural reliability of alumina-, feldspar-, leucite-, mica- and zirconia-based ceramics, J Dent 28 (2000), pp. 529–535. SummaryPlus | Full Text + Links | PDF (118 K) | View Record in Scopus | Cited By in Scopus (53)

2 W. Awliya, A. Odén, P. Yaman, J.B. Dennison and M.E. Razzoog, Shear bond strength of a resin cement to densely sintered high-purity alumina with various surface conditions, Acta Odontol Scand 56 (1998), pp. 9–13. Full Text via CrossRef

3 R. Scotti, S. Catapano and A. D'Elia, A clinical evaluation of In-Ceram crowns, Int J Prosthodont 8 (1995), pp. 320–323. View Record in Scopus | Cited By in Scopus (31)

4 A. Odén, M. Andersson, I. Krystek-Ondracek and D. Magnusson, Five-year clinical evaluation of Procera AllCeram crowns, J Prosthet Dent 80 (1998), pp. 450–456.

5 J. Tinschert, G. Natt, W. Mautsch, M. Augthun and H. Spiekermann, Fracture resistance of lithium disilicate-, alumina-, and zirconia-based three-unit fixed partial dentures: a laboratory study, Int J Prosthodont 4 (2001), pp. 231–238.

6 M. Hayashi, Y. Tsuchitani, Y. Kawamura, M. Miura, F. Takeshige and S. Ebisu, Eight-year clinical evaluation of fired ceramic inlays, Oper Dent 25 (2000), pp. 473–481. View Record in Scopus | Cited By in Scopus (28)

7 M. Fradeani and M. Redemagni, An 11-year clinical evaluation of leucite-reinforced glass-ceramic crowns: a retrospective study, Quintessence Int 33 (2002), pp. 503–510. View Record in Scopus | Cited By in Scopus (26)

8 P. Dérand and T. Dérand, Bond strength of luting cements to zirconium oxide ceramics, Int J Prosthodont 13 (2000), pp. 131–135.

9 M. Madani, F.C. Chu, A.V. McDonald and R.J. Smales, Effects of surface treatments on shear bond strengths between a resin cement and an alumina core, J Prosthet Dent 83 (2000), pp. 644–647. SummaryPlus | Full Text + Links | PDF (80 K) | View Record in Scopus | Cited By in Scopus (31)

10 M. Özcan, H. Alkumru and D. Gemalmaz, The effect of surface treatment on the shear bond strength of luting cement to a glass-infiltrated alumina ceramic, Int J Prosthodont 14 (2001), pp. 335–339.

11 A. Della Bona, K.J. Anusavice and C. Shen, Microtensile strength of composite bonded to hot-pressed ceramics, J Adhes Dent 2 (2000), pp. 305–313.

12 A. Della Bona and K.J. Anusavice, Microstructure, composition, and etching topography of dental ceramics, Int J Prosthodont 15 (2002), pp. 159–167.

13 K.J. Söderholm and S.W. Shang, Molecular orientation of silane at the surface of colloidal silica, J Dent Res 72 (1993), pp. 1050–1054.

14 N.M. Jedynakiewicz and N. Martin, The effect of surface coating on the bond strength of machinable ceramics, Biomaterials 22 (2001), pp. 749–752. SummaryPlus | Full Text + Links | PDF (469 K) | View Record in Scopus | Cited By in Scopus (8)

15 A. Della Bona, K.J. Anusavice and J.A. Hood, Effect of ceramic surface treatment on tensile bond strength to a resin cement, Int J Prosthodont 15 (2002), pp. 248–253.

16 T. Hooshmand, R. van Noort and A. Keshvad, Bond durability of the resin-bonded and silane treated ceramic surface, Dent Mater 18 (2002), pp. 179–188. SummaryPlus | Full Text + Links | PDF (1147 K) | View Record in Scopus | Cited By in Scopus (24)

17 S. Debnath, S.L. Wunder, J.I. McCool and G.R. Baran, Silane treatment effects on glass/resin interfacial shear strengths, Dent Mater 19 (2003), pp. 441–448. SummaryPlus | Full Text + Links | PDF (176 K) | View Record in Scopus | Cited By in Scopus (34)

18 A. Della Bona, C. Shen and K.J. Anusavice, Work of adhesion of resin on treated lithia disilicate-based ceramic, Dent Mater 20 (2004), pp. 338–344. SummaryPlus | Full Text + Links | PDF (230 K)

19 M. Kern and V.P. Thompson, Sandblasting and silica coating of a glass-infiltrated alumina ceramic: volume loss, morphology, and changes in the surface composition, J Prosthet Dent 71 (1994), pp. 453–461. SummaryPlus | Full Text + Links | PDF (1087 K) | View Record in Scopus | Cited By in Scopus (54)

20 M. Blixt, E. Adamczak, L.A. Lindén, A. Odén and K. Arvidson, Bonding to densely sintered alumina surfaces: effect of sandblasting and silica coating on shear bond strength of luting cements, Int J Prosthodont 13 (2000), pp. 221–226. View Record in Scopus | Cited By in Scopus (34)

21 R. Sun, N. Suansuwan, N. Kilpatrick and M. Swain, Characterisation of tribochemically assisted bonding of composite resin to porcelain and metal, J Dent 28 (2000), pp. 441–445. SummaryPlus | Full Text + Links | PDF (146 K) | View Record in Scopus | Cited By in Scopus (17)

22 S.M. Wegner, W. Gerdes and M. Kern, Effect of different artificial aging conditions on ceramic-composite bond strength, Int J Prosthodont 15 (2002), pp. 267–272. View Record in Scopus | Cited By in Scopus (22)

23 R. Van Noort, S. Noroozi, I.C. Howard and G. Cardew, A critique of bond strength measurements, J Dent 17 (1989), pp. 61–67. Abstract | View Record in Scopus | Cited By in Scopus (164)

24 A. Della Bona and R. Van Noort, Shear vs. tensile bond strength of resin composite bonded to ceramic, J Dent Res 74 (1995), pp. 1591–1596. View Record in Scopus | Cited By in Scopus (87)

25 P.H. DeHoff, K.J. Anusavice and Z. Wang, Three-dimensional finite element analysis of the shear bond test, Dent Mater 11 (1995), pp. 126–131. SummaryPlus | Full Text + Links | PDF (896 K) | View Record in Scopus | Cited By in Scopus (56)

26 J.J. Mecholsky Jr., Fractography: determining the sites of fracture initiation, Dent Mater 11 (1995), pp. 113–116. SummaryPlus | Full Text + Links | PDF (639 K) | View Record in Scopus | Cited By in Scopus (25)

27 A. Versluis, D. Tantbirojn and W.H. Douglas, Why do shear bond tests pull out dentin?, J Dent Res 76 (1997), pp. 1298–1307. View Record in Scopus | Cited By in Scopus (121)

28 S. Sudsangiam and R. van Noort, Do dentin bond strength tests serve a useful purpose?, J Adhes Dent 1 (1999), pp. 57–67. View Record in Scopus | Cited By in Scopus (61)

29 A. Della Bona, K.J. Anusavice and J.J. Mecholsky Jr., Failure analysis of resin composite bonded to ceramic, Dent Mater 19 (2003), pp. 693–699. SummaryPlus | Full Text + Links | PDF (537 K)

30 M. Kern and V.P. Thompson, Bonding to glass infiltrated alumina ceramic: adhesive methods and their durability, J Prosthet Dent 73 (1995), pp. 240–249. Abstract | PDF (4638 K) | View Record in Scopus | Cited By in Scopus (100)

31 M. Kern and S.M. Wegner, Bonding to zirconia ceramic: adhesion methods and their durability, Dent Mater 14 (1998), pp. 64–71. SummaryPlus | Full Text + Links | PDF (1842 K) | View Record in Scopus | Cited By in Scopus (80)

32 S.M. Wegner and M. Kern, Long-term resin bond strength to zirconia ceramic, J Adhes Dent 2 (2000), pp. 139–147. View Record in Scopus | Cited By in Scopus (51)

33 R. Friederich and M. Kern, Resin bond strength to densely sintered alumina ceramic, Int J Prosthodont 15 (2002), pp. 333–338. View Record in Scopus | Cited By in Scopus (21)

34 R. Frankenberger, N. Krämer and J. Sindel, Repair strength of etched vs silica-coated metal-ceramic and all-Ceramic restorations, Oper Dent 25 (2000), pp. 209–215. View Record in Scopus | Cited By in Scopus (27)

35 D.R. Haselton, A.M. Diaz-Arnold and J.J. Dunne Jr., Shear bond strengths of 2 intraoral porcelain repair systems to porcelain or metal substrates, J Prosthet Dent 86 (2001), pp. 526–531. Abstract | PDF (103 K) | View Record in Scopus | Cited By in Scopus (11)

36 R.M. Foxton, P.N. Pereira, M. Nakajima, J. Tagami and H. Miura, Durability of the dual-cure resin cement/ceramic bond with different curing strategies, J Adhes Dent 4 (2002), pp. 49–59. View Record in Scopus | Cited By in Scopus (19)

37 R. van Noort, G.E. Cardew, I.C. Howard and S. Noroozi, The effect of local interfacial geometry on the measurement of the tensile bond strength to dentin, J Dent Res 70 (1991), pp. 889–893. View Record in Scopus | Cited By in Scopus (93)

38 Y. Kitasako, M.F. Burrow, T. Nikaido, N. Harada, S. Inokoshi, T. Yamada and T. Takatsu, Shear and tensile bond testing for resin cement evaluation, Dent Mater 11 (1995), pp. 298–304. SummaryPlus | Full Text + Links | PDF (1741 K) | View Record in Scopus | Cited By in Scopus (36)

39 S. Phrukkanon, M.F. Burrow and M.J. Tyas, The influence of cross-sectional shape and surface area on the microtensile bond test, Dent Mater 14 (1998), pp. 212–221. SummaryPlus | Full Text + Links | PDF (714 K) | View Record in Scopus | Cited By in Scopus (70)

40 Y. Shono, M. Terashita, J. Shimada, Y. Kozono, R.M. Carvalho, C.M. Russel and D.H. Pashley, Durability of resin-dentin bonds, J Adhes Dent 1 (1999), pp. 211–218. View Record in Scopus | Cited By in Scopus (52)

41 K.K. Chen, Y. Shono, T. Ogawa, Y. Kozono and M. Terashita, Fracture aspects of resin-dentin bonding in non-trimming microtensile test, Dent Mater J 20 (2001), pp. 315–324. View Record in Scopus | Cited By in Scopus (4)

Reprint requests to: Dr Alvaro Della Bona, University of Passo Fundo, Campus I –Highway BR 285, PO Box 611, Passo Fundo, RS 99001-970, BRAZIL Fax: 01155-54-36-8403

The Journal of Prosthetic Dentistry Volume 93, Issue 3, March 2005, Pages 253-259

O efeito do tratamento da superfície cerâmica vinculada a cerâmica densamente sinterizada de alumina

Luiz Felipe Valandro DDS, MSca, Alvaro Della Bona DDS, MMedSci, PhDb,, Marco Antonio Bottino DDS, PhDc e Maximiliano Piero Neißer DDS, MSc, PhDd 
AProfessor, Reparadora Departamento de Odontologia, Faculdade de Odontologia da Universidade Federal de Santa Maria 
BProfessor e Coordenador da Investigação, Faculdade de Odontologia da Universidade de Passo Fundo 
CProfessor, Departamento de Materiais Dentários e Prostodontia, Sao Paulo State University em São José dos Campos 
DProfessor, Departamento de Materiais Dentários e Prostodontia, Sao Paulo State University em Sao Jose dos Campos 
Universidade Federal de Santa Maria, Rio Grande do Sul, Brasil; Universidade de Passo Fundo, Rio Grande do Sul, Brasil; Sao Paulo State University em São José dos Campos, Brasil. Disponível em linha 9 de Março de 2005.

Declaração do problema 
O tratamento superficial da cerâmica é crucial para a ligação à resina. Normalmente as cerâmicas são mal condicionadas usando os tradicionais procedimentos.

Finalidade 
O objetivo deste estudo foi avaliar o efeito da sílica em um revestimento de cerâmica densamente sinterizada por alumina em relação à força de união com o compósito, utilizando uma resina como agente de cimentação.

Material e métodos 
Foram feitos blocos (6 × 6 × 5 milímetros) de cerâmica e compósitos. A superfície das cerâmicas (Procera AllCeram) foram polidas, e os blocos foram divididos em 3 grupos (N = 5): SB, partículas atmosféricas - abrasão com 110 - µ m Al2O3; RS, sílica revestimento usando Rocatec System; E CS, sílica revestimento utilizando CoJet System. Os blocos de cerâmica foram tratados e cimentados nos blocos de compósito (W3D Master) utilizando um agente de cimentação a base de resina (Panavia F). Estes foram armazenados em água destilada a 37 ° C por 7 dias e, em seguida, cortados em 2 eixos, x e y, para obter amostras com uma área de superfície de aproximadamente 0,6 mm2 (N = 30). Os blocos foram submetidos a tensões em máquinas universais e se soltaram. Os dados foram analisados estatisticamente usando uma distribuição aleatória e através do Teste de Tukey (bis =. 05). As superfícies foram examinadas utilizando a microscopia óptica e microscopia eletrônica de varredura para determinar o tipo de falha.

Resultados 
Os valores da força de união (MPa) dos Grupos RS (17,1 ± 3,9) (P =. 00015) e CS (18,5 ± 4,7) (P =. 00012), foram significativamente mais elevados do que os valores do Grupo SB (12,7 ± 2,6). Não houve diferença estatística entre os Grupos RS e CS. Todas as falhas ocorreram na zona adesiva.

Conclusão 
Os sitemas com revestimento de sílica aumentaram a união entre o agente de cimentação Panavia F e a cerâmica Procera AllCeram. 


Artigo Outline 
Material e métodos 
Resultados 
Discussão 
Conclusões 
Referências 

Implicações clínicas 
Silica revestimento de cerâmica de alumina densamente sinterizada restaurações aumentou o vínculo forte com a resina luting agente testado. 
Com o aumento do teor de óxido de alumínio (Al2O3) em feldspathic cerâmica, registou - se uma melhoria significativa das propriedades mecânicas destes materiais, permitindo - metal - restaurações livre para ser utilizado mais predictably.1 Procera AllCeram (Nobel Biocare, Estocolmo, Suécia) É uma alta resistência com um caco muito densa, sinterizada Al2O3 conteúdo (99,9% de Al2O3), com um insignificante glassy phase.2 
A cerâmica com alto teor cristalino (alumínio e / ou zircónio óxidos), têm demonstrado resultados clínicos melhores do que feldspato -, leucite -, e lítio - Disilicato baseado ceramics.3, 4, 5, 6 e 7 De facto, o aumento da resistência mecânica, 
No entanto, a vinculação de resinas compostas de feldspato -, leucite -, e lítio - Disilicato baseado cerâmica está bem estabelecida. De ácido fluorídrico ataca o vidro fase produzindo um retention superfície para micromechanical caução, e as silane acoplamento agente químico promove um elo entre a sílica destas cerâmicas e os grupos metacrilato do resin.11, 12, 13, 14, 15, 16, 17 E 18 A sílica revestimento process9, 10, 14 e 16 é baseada em princípios semelhantes adesivos e parece ser um método promissor para o tratamento da alta cristalino cerâmica. 
Alguns estudos avaliaram o efeito da sílica acabamento do vínculo força de ácido - resistente cerâmica ligada à resina luting agents.2, 19, 20, 21 e 22 Além disso, vários autores têm criticado algumas obrigações força métodos e sugeriu a utilização de 
No entanto, poucas informações estão disponíveis sobre o efeito de vinculação sílica - revestidos alta cristalino cerâmica para resina luting agentes contendo fosfato monómeros. Portanto, o objetivo deste estudo foi testar a hipótese de que sílica - um revestimento de alumina densamente sinterizada cerâmica aumenta a força de um vínculo resina luting agente contendo fosfato monómeros.

Material e métodos 
Quinze blocos (6 milímetros × 6 milímetros × 5 milímetros) de cerâmica de alumina densamente sinterizada (Procera AllCeram (PR); Nobel Biocare, Göteborg, Suécia), foram obtidos a partir do fabricante. A cerâmica superfície foi polido com 1200 - Cascalho metallographic papel (3M ESPE, St. Paul, Minn) usando uma máquina polimento (Labpol 8-12; Extec, Enfield, Conn). Cada bloco cerâmico foi duplicada em resina composta (lote não. 010/03; W3D Master; Wilcos, Petrópolis, Brasil), utilizando um molde feito de um complemento Silicone impressão materiais (Elite HD, nenhum lote. Bo1.01.B; Zhermack, Badia Polesine, Rovigo, Itália). Incremental camadas de resina composta (2 milímetros) foram condensadas no molde e polymerized de 40 segundos (XL 3000; 3M ESPE; Luz da saída = 500 mW/cm2) para encher o molde. Uma das resinas compostas (RC) foi fabricado para cada bloco cerâmico bloco. 
Os blocos cerâmicos foram aleatoriamente divididos em 3 grupos e tratados como se segue. Pelo Grupo SB espécimes, a cerâmica superfície foi tratada através de um sistema de ar - partícula abrasão com 110 - µ m partículas de óxido de alumínio (MicroEtcher; Danville Engineering, San Ramon, Calif). A abrasão foi aplicada perpendicularmente à superfície a uma distância de 10 mm para 15 segundos e, a uma pressão de 2,8 bar. 
Pelo Grupo RS espécimes da Rocatec System (lote não. 363; 3M ESPE) foi utilizada para tratar a superfície cerâmica. As recomendações do fabricante foram seguidos para a utilização do Rocatec - Pre, Rocatec - Plus, e Rocatec - Sil. O Rocatec - Pre utiliza partículas atmosféricas - abrasão com 110 - µ m Al2O3 partículas empregam o mesmo abrasão parâmetros utilizados com o grupo SB. O Rocatec - Plus é constituído por partículas atmosféricas - abrasão usando 110 - µ m Al2O3 partículas modificadas por sílica com abrasão parâmetros igual ao Rocatec - Pre. O Rocatec - Sil foi aplicado para a sílica - revestidos surface.20, 30, 31, 32 e 33 
Para o Grupo CS cerâmica superfície foi tratada com partículas atmosféricas - abrasão com 30 - µ m Al2O3 partículas modificadas por sílica (CoJet System, nenhum lote. 118484; 3M ESPE), usando os mesmos parâmetros utilizados abrasão com a SB e RS Grupos. As superfícies foram revestidos com um silane acoplamento agente (ESPE - Sil; 3M ESPE), que foi autorizada a ar seco para 5 minutes.34 e 35 
Um exemplar de cada grupo adicional foi sputter - revestido com ouro - paládio (Hummer II Sputter Coater; Technics Inc, Alexandria, VA), para 3 minutos, em uma corrente de 10 mA, eo vácuo de 130 mTorr. A topografia da superfície espécimes foram analisados usando um microscópio eletrônico de varredura (JSM 6400; Jeol Ltd, Tóquio, Japão) .12 Alguns CoJet - tratados cerâmica espécimes foram analisados para o teor de sílica. Silica mapeamentos foram gerados usando espectroscopia de energia dispersiva (EDS), em 20 Kv. Representante imagens e espectros foram registrados. 
Cada bloco foi tratada cerâmica ligada a um bloco composto resina luting sistema usando um (lote não. 107AF, Dual - Cure Dental Adesivo Sistema Panavia F; Kuraray Co, Okayama, Japão), de acordo com as instruções do fabricante. A cerâmica - resina luting agente - compósito conjunto foi colocado sob uma carga de 750 gramas em uma coletiva de imprensa (EMIC PCE 10D; EMIC, São Jose dos Pinhais, Brazil) .30, 31, 32 e 33 O excesso de resina luting agente foi removido com Uma escova. A resina luting agente foi polymerized (XL 3000) por 40 segundos em cada um dos lados do block.36 An oxigênio inibidor (Oxyguard; Kuraray Co) foi aplicada sobre a camada de resina luting agente para 10 minutos antes de remover os blocos da imprensa. Os blocos foram lavados com ar - água pulverizada e armazenados em água destilada a 37 ° C por 7 dias. 
Os blocos foram dívida com cyanoacrylate (Super Bonder Gel; Loctite Ltda, São Paulo, Brasil), para um metal de base, que foi anexado a uma baixa velocidade, precisão corte automático máquina (Minitom; Struers, Copenhagen, Dinamarca) (Fig. 1 , A). Fatias de aproximadamente 0,8 mm de espessura foram obtidos através de um lento - velocidade diamante roda viu (lote não. 7016; KG Sorensen, Barueri, Brasil), sob refrigeração água (Fig. 1, B). O periférico fatias foram descartados, porque o resultado pode ser influenciado por qualquer um excesso ou uma quantidade insuficiente de resina luting agente no interface.11, 37 e 38 Nontrimmed espécimes foram obtidos diretamente com a máquina de corte, o que significa que nem polimento nem acabamento foi realizado. Este procedimento foi utilizado para evitar estresse concentração no adesivo Interface por polimento com materiais diferentes elástica moduli.11 Six nontrimmed barra em forma de amostras com uma caução área de aproximadamente 0,6 mm2 foram obtidos por bloco (N = 30) (Fig. 2 , B) .11, 39, 40 e 41 
  
Display Full Size versão desta imagem (15K) 
Fig. 1. Um, o bloco foi colada de metal básico acompanha a máquina de corte. B, três fatias (± 0,8 mm de espessura) foram obtidos por bloco. 
  
Display Full Size versão desta imagem (16K) 
Fig. 2. (A) As fatias foram cortadas; (B) 6 interior espécimes foram utilizados para tracção vínculo força testes. Asterisk indica adesivo zona como descrito por Della Bona e al.11 
Os espécimes foram colados com cyanoacrylate a um calibrador adaptado, paralelamente ao seu longo eixo, minimizando assim a dobra forças na zona adesivo durante microtensile testes. Este aparelho foi ligado a uma máquina universais ensaio (EMIC DL - 1000; EMIC), e os espécimes foram carregados na tensão de falha em um crosshead parafuso velocidade de 1 mm/min.11 e 40 
Bond força (σ) valores foram calculados utilizando σ = L / A, onde L é a carga em um fracasso e é o adesivo área medido utilizando um calibrador digitais (Mitutoyo, Tóquio, Japão) antes de testing.11 Os resultados foram analisados utilizando Randomizado um bloco completo desenho análise de variância (ANOVA) e Tukey do teste (bis =. 05) e software estatístico (Statistix 8,0 para Windows; Analytical Software Inc, Tallahassee, Fla). Fractured superfícies foram observados usando luz microscopia (Zeiss MC 80 DX; Carl Zeiss, Jena, Alemanha) e digitalização microscopia eletrônica (SEM) (JEOL - JSM - T330A; Jeol Ltd) para determinar o tipo de falha, que foi classificada como coesa ou Adesivo no âmbito de qualquer dos substratos ou interface.

Resultados 
O desenho randomizado completa bloco ANOVA é descrito na Tabela I, mostrando que houve diferenças significativas entre os grupos. A média de títulos e valores força desvios padrão são apresentados na Tabela II. A média dos valores vínculo força Grupos RS e CS não foram significativamente diferentes (P =. 25), mas os valores médios dos dois grupos foram significativamente mais elevados do que o valor médio do Grupo SB (P =. 0001). Representante SEM imagens dos tratados Procera AllCeram cerâmica espécimes são mostradas na Figura 3. Exame da cerâmica superfícies tratadas com ambos Rocatec - Plus e CoJet - Sand (Fig. 3) mostrou uma deposição de partículas para a superfície, que foi diferente do observado na superfície áspera espécimes do Grupo SB (Fig. 3, A) . Figura 3, D, mostra um mapeamento sílica imagem baseada na EDS análise da superfície de sílica - revestidos Procera AllCeram. A análise das superfícies fraturadas revelou que todas as falhas ocorreram na zona adesiva. Todas as falhas foram coesa fraturas na resina luting agente - cerâmicos Interface (Fig. 4, Fig. 5 e Fig. 6). 
Quadro I. 
Randomized completa bloco concepção ANOVA 
Source SS df MS FPR577.7315.547B484.321.074r × B20418.8920.944Surface tratamento 2550 .76 275,378 22.36.0001Error58714.3012.315Total891845.98df, graus de liberdade; SS, soma quadrados; MS, Quadrático médio; B, bloco; R - repetições. 
Quadro II. 
Mean vínculo força valores e desvio padrão (MPa) dos grupos experimentais e valor crítico de comparação 
SB RS CSTukeyMean valores * 12.7a17.1b18.5b3.402Standard desvio 2,6 3,9 4,7 SB, Airborne - partícula abrasão com 110 - µ m Al2O3; RS, sílica revestimento usando Rocatec System; CS, sílica revestimento usando CoJet System. 
* Diferentes superscritos cartas indicam diferença estatística, P <.05. 
  
Display Full Size versão desta imagem (201K) 

Fig. 3. Representante SEM imagens de cerâmica superfícies tratadas: A, partículas atmosféricas - abrasão com 110 - µ m Al2O3, cerâmica tratamentos superficiais utilizados para espécimes do grupo SB (originais Ampliação × 2000); B, sílica utilizando Rocatec Sistema de revestimento, cerâmica tratamentos superficiais utilizados para espécimes No Grupo RS (originais Ampliação × 2000); C, sílica revestimento usando CoJet System, cerâmica tratamentos superficiais utilizados para espécimes no Grupo CS (originais Ampliação × 2000); D, EDS sílica mapeamento de sílica - superfície de revestimento cerâmico Grupo CS; Manchas brancas são sílica (originais Ampliação × 100). 
  
Display Full Size versão desta imagem (95K) 

Fig. 4. Representante SEM imagens da superfície de espécimes fraturados do Grupo SB. Espaço dentro da casa branca (A) é ampliada em B (asterisco representa resina cimento; Espada símbolo representa cerâmica) (originais magnifications: A, × 100; B, × 5000). 
  
Display Full Size versão desta imagem (90K) 

Fig. 5. Representante SEM imagens da superfície de espécimes fraturados do Grupo RS. Espaço dentro da casa branca (A) é ampliada em B (asterisco representa resina cimento; Espada símbolo representa cerâmica) (originais magnifications: A, × 100; B, × 5000). 
  
Display Full Size versão desta imagem (86K) 

Fig. 6. Representante SEM imagens da superfície de espécimes fraturados do Grupo CS. Espaço dentro da casa branca (A) é ampliada em B (asterisco representa resina cimento; Espada símbolo representa cerâmica) (originais magnifications: A, × 100; B, × 5000). 
Discussão 
Os resultados deste estudo confirmou a hipótese de que uma sílica revestimento de alumina densamente sinterizada cerâmica aumenta a força de um vínculo resina luting agente contendo fosfato monómeros. Quando uma investigação científica propõe - se testar o vínculo entre um adesivo e um aderente, um dos elementos essenciais é o método utilizado para medir a força obrigacionista na interface. In vitro, vínculo força testes, como a tracção ou cisalhamento testes, têm por base a aplicação de uma carga de gerar estresse no espécimes até fratura ocorra. Daí, para o ensaio vínculo força suficiente para produzir valores entre um sistema adesivo e um substrato, é fundamental que a vinculação Interface ser o mais salientou região, independentemente de o teste ser employed.23, 24, 25 e 27 
Muitos pesquisadores, usando estresse distribuição análises, têm relatado que alguns títulos força testes não adequadamente salientar a interfacial zone.23, 24, 25, 27, 28 e 38 Com efeito, cisalhamento testes foram criticadas para o desenvolvimento de nonhomogeneous estresse nas distribuições A ligação da relação, induzindo tanto uma subestimação ou uma má interpretação dos resultados, uma vez que o fracasso muitas vezes começa em um dos substratos e não ao adesivo zone.23, 24, 25, 27, 28 e 38 
Embora convencional tracção testes também apresentar algumas limitações, como a dificuldade de espécime alinhamento e à tendência de um heterogêneo estresse distribuição no adesivo Interface, 23 e 38 deste tipo de teste pode ser utilizado, uma vez que fornece informações sobre o conjunto vínculo strength.15 , 16 e 41 The microtensile ensaio, por outro lado, permite que para um alinhamento adequado dos espécimes, bem como uma distribuição mais homogênea de stress, para além de uma maior sensibilidade comparação ou avaliação de títulos fortes que são similar.11 Como todos de Os espécimes falharam dentro da zona adesiva, os valores médios são relatados representante medições da tensão vínculo forte para os materiais studied.11 e 29 
Baseada em Della Bona et al - 11 a aderência na zona deste estudo consiste no seguinte: a interfacial região entre a resina luting agente e as resinas compostas dentro do qual moleculares e interação química vinculação ocorrer, a resina luting agente, e os interfacial região entre A resina luting agente e da cerâmica dentária. Esta última inclui a superfície região tratados com ar - partícula abrasão e / ou revestidos com sílica partículas e silane tal que micromechanical e / ou químicas vinculação ocorre (Fig. 2, B). 
Fracture superfícies foram examinadas utilizando luz e microscopia eletrônica varredura. SEM análise fornecido informações mais detalhadas sobre os acontecimentos do que a fratura microscopia óptica. Representante fratura superfícies são mostrados na Fig. 4, Fig. 5 e Fig. 6. Verifica - se que o tipo de falha para todos os grupos foi semelhante. Coesa fratura ocorreu sempre dentro da zona adesiva na resina luting agente - cerâmicos relação. No entanto alguns autores sugerem que fractographic análise da fratura superfícies fornece informações qualitativas sobre o processo fratura e deve acompanhar o vínculo força studies.11, 15, 26 e 29 
O tribochemical sílica sistemas de pintura aumentou o vínculo forte entre o caco e da resina luting agente estudado. Esse resultado pode ser explicado por 3 mecanismos: a criação de um padrão topográfico permitindo a micromechanical vinculação a resina; A química vínculo entre a sílica - revestido e cerâmica superfície do silane agente (y - methacryloxypropyltrimethoxysilane), e os segundos para a resina materiais; E da química vínculo entre o fosfato monómeros MDP (10 - methacryloxydecyl - dihidrogenofosfato - fosfato) e do alumínio oxides.32 Tanto o Rocatec (Fig. 3, B) e ao CoJet (Fig. 3, C) sistemas produziu uma sílica - revestidos Cerâmica superfície, o que foi confirmado utilizando sílica mapeamento (Fig. 3, D). A sílica sistemas de pintura criou uma camada de sílica sobre a superfície cerâmica, devido à alta velocidade superfície impacto das partículas de alumina modificada pela sílica. Foi relatado que a atmosfera partículas podem penetrar até 15 µ m para a cerâmica e metal substrates.21 
Kern e Thompson19 observado um aumento do teor de sílica na superfície do In - Ceram cerâmica, de 15,8% para 19,7%, após o tratamento com o Rocatec - Plus sistema, sugerindo que este tratamento superficial poderia melhorar o vínculo força de Resina, o que mais tarde foi relatada por outras studies.8, 10 e 30 O CoJet e os Rocatec sistemas utilizam métodos semelhantes para revestimento de sílica. O CoJet é um método mais versátil para procedimentos clínicos, tais como a reparação directa de metais fraturado - cerâmica e metal - livres utilizando cerâmica restaurações de resina composta, e cimentação adesiva. O Rocatec sistema é mais adequado para uso laboratorial. No entanto, ambos os sistemas empregam silicatization e silanization do substrate.34 e 35 Alguns estudos indicaram que a média vínculo força valores de vidro - infiltradas aluminous cerâmica ligada à resina aumentou após sílica - revestimento, em comparação com partículas atmosféricas - abrasão com Al2O3 partículas ou hydrofluoric Ácido treatments.2, 8, 9 e 10 
As cerâmicas podem ser classificadas como quer ácido - sensíveis ou ácido - resistente, de acordo com o grau de degradação com superfície de ácido fluorídrico (HF). Ácido - sensíveis cerâmica, feldspato -, leucite - e lítio - Disilicato baseado cerâmica, são rapidamente gravado por HF, resultando em micromechanical retention cerâmica superfícies. Ácido - resistente cerâmica, vidro - cerâmica infiltrada alumina e zircónia sistemas, de alumina densamente sinterizada cerâmica, e óxido de ítrio - - - parcialmente estabilizada zircónia cerâmicas não demonstram grande superfície degradação por HF gravação, impedir um fiável micromechanical vínculo de resina. 
A química vínculo para substratos cerâmicos pode, portanto, ser determinada pela presença de sílica na cerâmica composition.14 Embora ácidos sarge principalmente a glassy fase, eliminando alguns sílica a partir da superfície para criar um retention topografia para micromechanical caução não interfere com silanes Produção de um produto químico vínculo com o restante silica.14 Além disso, a silane é bifuncional, também promover um produto químico vínculo para resinous materiais através de um cruzamento - articulação com metacrilato grupos. Most silane acoplamento agentes também aumentar o substrato superfície da energia e melhorar a superfície wettability para resins.11, 12, 13, 14, 15, 16, 17 e 18 A sílica - silane química vínculo pode ocorrer com ácido - resistente cerâmicas, desde que o Sílica revestimento da superfície cerâmica é utilizada. Kern e Thompson16 observou que a silane de Rocatec - Sil produzido um produto químico para um vínculo de sílica - revestidos de vidro - infiltradas caco de alumina (In - Ceram). Essa caução foi insignificante sílica sem revestimento, o que sugere que silicatization e silanization procedimentos são essenciais para promover a ligação entre resina e do In - Ceram cerâmica. 
O Procera AllCeram caco contém 99% de óxido de alumínio, caracterizando um ácido - resistente ceramic.2, 20 e 33 No entanto, outros estudos de ácido - resistente cerâmica ligada às resinas relatados valores superiores vínculo força quando uma resina luting agente contendo fosfato monómeros foi usado , O que corrobora os resultados do presente estudo, sugerindo que a associação de sílica revestimento, silanization, e resinas contendo fosfato monómeros produziu o maior vínculo força valores de ácido - resistente cerâmicos ligada ao resin.10, 22, 30, 31, 32 E 33 Os resultados são relevantes para os materiais e procedimentos usados no presente estudo. Futuros estudos deverão analisar o efeito da sílica acabamento do vínculo força para outras de alto teor cristalino cerâmica. 
Conclusões 
Tribochemical sílica sistemas de pintura (Rocatec e CoJet) aumentou significativamente a força valores significam vínculo entre um caco de alumina densamente sinterizada (Procera AllCeram) e uma resina luting agente contendo fosfato monómeros, confirmando o estudo hipótese. 

Referências 
1 J. Tinschert, D. Zwez, R. Marx e K.J. Anusavice, Structural confiabilidade de alumina -, feldspato -, leucite - de - mica e zircónia - com base cerâmica, J Dent 28 (2000), págs. 529-535. SummaryPlus | Full Text + Links | PDF (118 K) | View Record no Scopus | Citado por em Scopus (53) 
2 W. Awliya, A. Odén, P. Yaman, J. B. Dennison e M. E. Razzoog, Shear vínculo força de uma resina ao cimento densamente sinterizada alta pureza de alumina com diferentes condições superfície, Acta Odontol Scand 56 (1998 ), Págs. 9-13. Texto integral através crossref 
3 R. Scotti, S. Catapano e A. D'Elia, A avaliação clínica do In - Ceram coroas, Int J Prosthodont 8 (1995), págs. 320-323. View Record no Scopus | Citado por em Scopus (31) 
4 A. Odén, M. Andersson, I. Krystek - Ondracek e D. Magnusson, Cinco anos de avaliação clínica do Procera AllCeram coroas, J Prosthet Dent 80 (1998), págs. 450-456. 
5 J. Tinschert, G. Natt, W. Mautsch, M. Augthun e H. Spiekermann, Fracture resistência de lítio Disilicato -, de alumina -, e zircónia - baseado três unidades fixas parciais dentadura: um estudo laboratorial, Int J Prosthodont 4 (2001), págs. 231-238. 
6 M. Hayashi, Y. Tsuchitani, Y. Kawamura, M. Miura, F. Takeshige e S. Ebisu, oito anos de avaliação clínica de despedidas cerâmica inlays, Oper Dent 25 (2000), págs. 473-481. View Record no Scopus | Citado por em Scopus (28) 
7 M. Fradeani e M. Redemagni, An 11 anos de avaliação clínica de leucite - reforçado vidro - cerâmica coroas: um estudo retrospectivo, Quintessence Int 33 (2002), págs. 503-510. View Record no Scopus | Citado por em Scopus (26) 
8 P. Dérand e T. Dérand, Bond força da luting cimentos de óxido de zircónio cerâmica, Int J Prosthodont 13 (2000), págs. 131-135. 
9 M. Madani, F.C. Chu, A.V. McDonald e R.J. Smales, Efeitos de tratamentos superficiais sobre cisalhamento fortes vínculo entre uma resina cimento e um núcleo de alumina, J Prosthet Dent 83 (2000), págs. 644-647. SummaryPlus | Full Text + Links | PDF (80 K) | View Record no Scopus | Citado por em Scopus (31) 
10 M. Özcan, H. Alkumru e D. Gemalmaz, o efeito do tratamento superficial sobre o corte de luting cimento vínculo força de um copo - infiltradas de alumina cerâmica, Int J Prosthodont 14 (2001), págs. 335-339. 
11 A. Della Bona, K.J. Anusavice e C. Shen, Microtensile resistência dos compósitos ligada a quente - pressionado cerâmica, J Adhes Dent 2 (2000), págs. 305-313. 
12 A. Della Bona e K.J. Anusavice, Microestrutura, composição, topografia e gravação de dentista cerâmica, Int J Prosthodont 15 (2002), págs. 159-167. 
13 K.J. Söderholm e S.W. Shang, Molecular orientação do silane na superfície de sílica coloidal, J Dent Res 72 (1993), págs. 1050-1054. 
14 N. M. Jedynakiewicz e N. Martin, o efeito do revestimento na superfície vínculo força da maquinável cerâmica, Biomaterials 22 (2001), págs. 749-752. SummaryPlus | Full Text + Links | PDF (469 K) | View Record no Scopus | Citado por em Scopus (8) 
15 A. Della Bona, K.J. Anusavice e J.A. Hood, Efeito de cerâmica tratamento superficial sobre tracção vínculo força a uma resina cimento, Int J Prosthodont 15 (2002), págs. 248-253. 
16 T. Hooshmand, R. Van Noort e A. Keshvad, Bond durabilidade da resina - ligado e silane tratados cerâmica superfície, Dent Mater 18 (2002), págs. 179-188. SummaryPlus | Full Text + Links | PDF (1147 K) | View Record no Scopus | Citado por em Scopus (24) 
17 S. Debnath, S.L. Wunder, J.I. McCool e G.R. Baran, Silane tratamento efeitos sobre vidro / resina interfacial cisalhamento fortes, Dent Mater 19 (2003), págs. 441-448. SummaryPlus | Full Text + Links | PDF (176 K) | View Record no Scopus | Citado por em Scopus (34) 
18 A. Della Bona, C. Shen e K.J. Anusavice, Trabalho de aderência da resina sobre tratados lithia Disilicato de base cerâmica, Dent Mater 20 (2004), págs. 338-344. SummaryPlus | Full Text + Links | PDF (230 K) 
19 M. Kern e V.P. Thompson, Sandblasting e sílica revestimento de um vidro - cerâmica de alumina infiltrada: Volume perda, morfologia, e mudanças na composição da superfície, J Prosthet Dent 71 (1994), págs. 453-461. SummaryPlus | Full Text + Links | PDF (1087 K) | View Record no Scopus | Citado por em Scopus (54) 
20 M. Blixt, E. Adamczak, L. A. Lindén, A. Odén e K. Arvidson, Bonding a densamente sinterizada Alumina superfícies: efeito do sandblasting e sílica revestimento em cisalhamento vínculo de luting cimentos força, Int J Prosthodont 13 (2000 ), Págs. 221-226. View Record no Scopus | Citado por em Scopus (34) 
21 R. Sun, N. Suansuwan, N. Kilpatrick e M. Swain, Caracterização de tribochemically assistida vinculação dos compostos de resina de porcelana e metal, J Dent 28 (2000), págs. 441-445. SummaryPlus | Full Text + Links | PDF (146 K) | View Record no Scopus | Citado por em Scopus (17) 
22 S.M. Wegner, W. Gerdes e M. Kern, Efeito de diferentes condições artificiais envelhecimento em cerâmica - compósito vínculo força, Int J Prosthodont 15 (2002), págs. 267-272. View Record no Scopus | Citado por em Scopus (22) 
23 R. Van Noort, S. Noroozi, I.C. Howard e G. Cardew, A crítica do vínculo força medições, J Dent 17 (1989), págs. 61-67. Abstract | View Record no Scopus | Citado por em Scopus (164) 
24 A. Della Bona e R. Van Noort, Shear vs força de tracção vínculo resinas compostas ligadas à cerâmica, J Dent Res 74 (1995), págs. 1591-1596. View Record no Scopus | Citado por em Scopus (87) 
25 P.H. DeHoff, K.J. Anusavice e Z. Wang, três dimensões elementos finitos análise do vínculo cisalhamento ensaio, Dent Mater 11 (1995), págs. 126-131. SummaryPlus | Full Text + Links | PDF (896 K) | View Record no Scopus | Citado por em Scopus (56) 
26 J.J. Mecholsky Jr., Fractography: determinação dos sítios de fratura início, Dent Mater 11 (1995), págs. 113-116. SummaryPlus | Full Text + Links | PDF (639 K) | View Record no Scopus | Citado por em Scopus (25) 
27 A. Versluis, D. Tantbirojn e W.H. Douglas, Por que cisalhamento vínculo testes puxe dentina? , J Dent Res 76 (1997), págs. 1298-1307. View Record no Scopus | Citado por em Scopus (121) 
28 S. Sudsangiam e R. Van Noort, Do dentina vínculo força testes servir a sua utilidade? , J Adhes Dent 1 (1999), págs. 57-67. View Record no Scopus | Citado por em Scopus (61) 
29 A. Della Bona, K.J. Anusavice e J.J. Mecholsky Jr., Failure análise de resinas compostas ligadas à cerâmica, Dent Mater 19 (2003), págs. 693-699. SummaryPlus | Full Text + Links | PDF (537 K) 
30 M. Kern e V.P. Thompson, de vidro Bonding infiltradas de alumina cerâmica: adesivos e os seus métodos durabilidade, J Prosthet Dent 73 (1995), págs. 240-249. Abstract | PDF (4638 K) | View Record no Scopus | Citado por em Scopus (100) 
31 M. Kern e S.M. Wegner, Bonding ao zircónia cerâmica: aderência e os seus métodos durabilidade, Dent Mater 14 (1998), págs. 64-71. SummaryPlus | Full Text + Links | PDF (1842 K) | View Record no Scopus | Citado por em Scopus (80) 
32 S.M. Wegner e M. Kern, a longo prazo resina vínculo força para zircónia cerâmica, J Adhes Dent 2 (2000), págs. 139-147. View Record no Scopus | Citado por em Scopus (51) 
33 R. Friederich e M. Kern, Resina vínculo à força de alumina densamente sinterizada cerâmica, Int J Prosthodont 15 (2002), págs. 333-338. View Record no Scopus | Citado por em Scopus (21) 
34 R. Frankenberger, N. Krämer e J. Sindel, Repair força da gravado versus sílica - metálicos revestidos - cerâmica e todos - Ceramic restaurações, Oper Dent 25 (2000), págs. 209-215. View Record no Scopus | Citado por em Scopus (27) 
35 D.R. Haselton, A.M. Diaz - Arnold e J.J. Dunne Jr., Shear vínculo dosagens de 2 intra porcelana reparar sistemas de porcelana ou metal substratos, J Prosthet Dent 86 (2001), págs. 526-531. Abstract | PDF (103 K) | View Record no Scopus | Citado por em Scopus (11) 
36 R.M. Foxton, P.N. Pereira, M. Nakajima, J. Tagami e H. Miura, Durabilidade da dupla - cura de resina cimento / cerâmica vínculo com diferentes estratégias cura, J Adhes Dent 4 (2002), págs. 49-59. View Record no Scopus | Citado por em Scopus (19) 
37 R. Van Noort, G.E. Cardew, I.C. Howard e S. Noroozi, o efeito dos locais interfacial geometria sobre a medição da força de tracção vínculo dentina, J Dent Res 70 (1991), págs. 889-893. View Record no Scopus | Citado por em Scopus (93) 
38 Y. Kitasako, M.F. Burrow, T. Nikaido, N. Harada, S. Inokoshi, T. Yamada e T. Takatsu, Shear e tracção vínculo testes para avaliação de resina cimento, Dent Mater 11 (1995), págs. 298-304. SummaryPlus | Full Text + Links | PDF (1741 K) | View Record no Scopus | Citado por em Scopus (36) 
39 S. Phrukkanon, M.F. Burrow e M. J. Tyas, A influência da Secção transversal forma ea superfície sobre a microtensile vínculo teste, Dent Mater 14 (1998), págs. 212-221. SummaryPlus | Full Text + Links | PDF (714 K) | View Record no Scopus | Citado por em Scopus (70) 
40 Y. Shono, M. Terashita, J. Shimada, Y. Kozono, R.M. Carvalho, C.M. Russel e D. H. Pashley, Durabilidade de resina - dentina obrigações, J Adhes Dent 1 (1999), págs. 211-218. View Record no Scopus | Citado por em Scopus (52) 
41 K.K. Chen, Y. Shono, T. Ogawa, Y. Kozono and M. Terashita, Fracture aspects of resin-dentin bonding in non-trimming microtensile test, Dent Mater J 20 (2001), pp. 315–324. View Record in Scopus | Cited By in Scopus (4) 


  Reprint requests to: Dr Alvaro Della Bona, University of Passo Fundo, Campus I –Highway BR 285, PO Box 611, Passo Fundo, RS 99001-970, BRAZIL Fax: 01155-54-36-8403 



The Journal of Prosthetic Dentistry 
Volume 93, Issue 3, March 2005, Pages 253-259